8 mm Rockpanel Lines² S & XL

A Rockpanel product with a shiplap profile that is suitable for soffit and fascia applications.   The material is fixed with a special clip which allows a dismountable and hidden fixing.  The material is available in 10 colours with an option of a primed board to receive site decoration; also a Natural finish is available.  The maximum lead time is 2 weeks.

8 mm Rockpanel Lines² can only be used in ventilated constructions.

950 FASCIAS/BARGES/SOFFITS: PRE-FINISHED STONEWOOL BOARD:

(Please delete clauses in red to suit specification)

Product reference: 8 mm Rockpanel Lines² S & XL

Material: Inert Rockwool panels with pre-finished decorative coating

Manufacturer: Rockwool BV / Lapinus, Industrieweg 15

6045 JG Roermond, The Netherlands

Sales Representative: Rockwool BV / Rockpanel Group, Wern Tarw, Pencoed, Bridgend CF35 6NY.

Tel:01656 863210.  Fax: 01656 863611.

E-mail: info@rockpanel.co.uk. Web: www.rockpanel.co.uk.

Board thickness: 8mm

Finish: Standard

Board dimensions:

S: 3050 x 164 mm wide

(Working width = 151 by fixed mounting and 156 by dismountable mounting)

XL: 3050 x 295 mm wide

(Working width = 182 by fixed mounting and 287 by dismountable mounting)

Colour:

Pure White RAL 9010 / Light Ivory RAL 1015 / Cream White RAL 9001 / Signal grey RAL 7004  / Anthracite Grey RAL 7016 / Primed finish / Natural

Accessories:

### External Corner Treatment

Rockpanel profile D: External corner profile (aluminium) for 10 mm board (2mm extra thickness of the corner profile is required due to the application of the mounting clip).

Colour: Colour matched to board / Black / White.

Manufacturer/ Distributor:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ.

Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Other requirements:

By mounting 8 mm Rockpanel Lines² No gaskets are required, providing fascia board extends 7.5mm beyond the soffit board.

Construction: 8 mm Rockpanel Lines² can only by used in ventilated and well drained constructions.

Board joints:	Fascias & soffits – At vertical wooden battens the material can be butt jointed up to a maximum length of 15M, then maintain a 10mm gap or alternatively maintain a 3mm gap on every length.

Junction of the soffit board and the fascia maintain a gap of 5mm.

Junction of Soffit and Wall: Maintain a 5mm gap.

Support:

50mm x 38mm softwood timber at maximum 500mm centres with 75 x 38mm timber at vertical board joints. All timber to be treated to Clause G20 270

Fixings:

8 mm Rockpanel Lines² will be fixed with a special Rockpanel clip which will be screw fixed with an accompanying screw. Please consult Rockpanel BV for wind loading calculations

270 Ungraded Softwood for Fascia, Soffit and Barge supports.

- Quality of timber: free from decay, insect attack (except pinhole borers) and with no knots wider than half the width of the section.

- Surface finish: PSE

- Treatment: C2